Ionic high-pressure form of elemental boron

Artem R. Oganov1,2,10, Jiuhua Chen3,4, Carlo Gatti5, Yanzhang Ma6, Yanming Ma1,7, Colin W. Glass1, Zhenxian Liu8, Tony Yu3, Oleksandr O. Kurakevych9, Vladimir L. Solozhenko9

1 Laboratory of Crystallography, Department of Materials, ETH Zurich, Wolfgang-Pauli-Str. 10, CH-8093 Zurich, Switzerland.

2 Geology Department, Moscow State University, 119992 Moscow, Russia.

3 Center for the Study of Matters at Extreme Conditions and Department of Mechanical and Materials Engineering, Florida International University, Miami, FL 33199, USA

4 Mineral Physics Institute and Department of Geosciences, Stony Brook University, Stony Brook, NY 11794-2100, USA

5 CNR-ISTM Istituto di Scienze e Tecnologie Molecolari, via Golgi 19, 20133 Milano, Italy.

6 Department of Mechanical Engineering, Texas University of Technology, 7th St. & Boston Ave., Lubbock, Texas 79409, USA.

7 National Lab of Superhard Materials, Jilin University, Changchun 130012, P. R. China.

8 Geophysical Laboratory, Carnegie Institution of Washington, Washington, DC 20015, USA

9 LPMTM-CNRS, Université Paris Nord, Villetaneuse, F-93430, France

10 Department of Geosciences and New York Center for Computational Science, Stony Brook University, Stony Brook, NY 11794-2100, USA.

Boron is an element of fascinating chemical complexity. Controversies have shrouded this element since its discovery was announced in 1808: the new ‘element’ turned out to be a compound containing less than 60–70%of boron, and it was not until 1909 that 99% pure boron was obtained. And although we now know of at least 16 polymorphs, the stable phase of boron is not yet experimentally established even at ambient conditions. Boron’s complexities arise from frustration: situated between metals and insulators in the periodic table, boron has only three valence electrons, which would favour metallicity, but they are sufficiently localized that insulating states emerge. However, this subtle balance between metallic and insulating states is easily shifted by pressure, temperature and impurities. Here we report the results of high-pressure experiments and ab initio evolutionary crystal structure predictions that explore the structural stability of boron under pressure and, strikingly, reveal a partially ionic high-pressure boron phase. This new phase is stable between 19 and 89 GPa, can be quenched to ambient conditions, and has a hitherto unknown structure (space group Pnnm, 28 atoms in the unit cell) consisting of icosahedral B12 clusters and B2 pairs in a NaCl-type arrangement. We find that the ionicity of the phase affects its electronic bandgap, infrared adsorption and dielectric constants, and that it arises from the different electronic properties of the B2 pairs and B12 clusters and the resultant charge transfer between them.

Reference:

Oganov A.R., Chen J., Gatti C., Ma Y.-Z., Ma Y.-M., Glass C.W., Liu Z., Yu T., Kurakevych O.O., Solozhenko V.L. (2009). Ionic high-pressure form of elemental boron. Nature 457, 863-867.

Acknowledgements:

ARO gratefully acknowledges the Swiss National Science Foundation (grant 200021-111847/1) and the ETH Research Equipment Programme for financial support of this work. Work of JC and TY is supported by the NSF (grant EAR0711321) and DOE (contract DE-FG02-07ER46461), work of YZM is funded by DOE (agreement DE-FC03-03NA00144) and NSF (grant DMR-0619215), work of OOK and VLS is supported by the Agence Nationale de la Recherche (grant ANR-05-BLAN-0141). Visualisations were done with the STM4 code developed by M. Valle. Calculations were performed at CSCS (Manno), Joint Supercomputer Centre of the Russian Academy of Sciences, and ETH Zurich.  The use of the NSLS at Brookhaven National Laboratory was supported by the US Department of Energy under contract DE-AC02-98CH10886, and the high-pressure beamlines U2A and X17C at the NSLS were supported by COMPRES under NSF Cooperative Agreement EAR 06-49658.